## Slide 1
Sugaren Co., Ltd. #410, 2 Gwahakgwan, 119. Dandae-ro, Dongnam-gu, Cheonan-si, Chungcheongnam-do, 330-714, Korea
www.sugaren.co.kr
Tel. 041-529-6262
Fax. 041-559-7954
E-mail: sugaren@sugaren.co.kr
Analytical Report
Analytical results
Information
의뢰기관 | -
분석시료명 | Pine tree (Korea)
분석항목 | Total
Components |  | Composition (wt.%) |  | 
Structural carbohydrates | Glucan |  | 41.09±0.28 | 
 | Xylan |  | 12.52±0.16 | 
 | Mannan |  | 3.12±0.15 | 
 | Galactan |  | 1.08±0.11 | 
 | Arabinan |  | 0.52±0.09 | 
 |  | Subtotal | 58.33 | 
Lignin | Acid soluble |  | 8.57±0.49 | 
 | Acid insoluble |  | 23.46±0.38 | 
 |  | Subtotal | 32.03 | 
Extractives | Water |  | 5.82±0.13 | 
 | EtOH |  | 1.29±0.09 | 
 |  | Subtotal | 7.11 | 
Acetyl group |  |  | 5.98±0.11 | 
Ash |  |  | 1.22±0.01 | 
Total |  |  | 104.67 | 
본 성적서는 의뢰자가 제공한 시료의 분석 결과이며, 당 사의 사전 동의 없이 상업적 목적으로 하는 선전, 광고 및 법적자료로 사용될 수 없습니다.
Quantification was performed by following NREL laboratory analytical procedures: NREL/TP510-42618 (structural carbohydrates and lignin), NREL/TP510-42619 (Extractives), NREL/TP510-42622 (ash) and NREL/TP-510-42625 (protein).
Multi-replication have been conducted for test assay in carbohydrate (n=25). Q-Test was used to identify statistical outliers in data. Q-Test decision level at 95% confidence interval for N=25 is 0.317.
Analyzed by : Won Il Choi
Approved by : Hyun Jin Ryu
(sign)
2017년 06월 00일
주식회사 슈가엔