## Slide 1
Product information: Lot No. FMPT
Product type | Saccharomate Fractomass
Source Biomass | Pine tree (Korea)
Fractionation | H2SO4–catalyzed hydrothermal process
Data Report
Ⓡ
Ⓡ
Sugaren Co., Ltd. #B207, Seogwan, 152, jukjeon-ro, Suji-gu, Yongin-si, Gyeonggi-do, 16890, Korea
www.sugaren.co.kr
Tel. 031-8005-3549
Fax. 031-8021-7420
E-mail: sugaren@sugaren.co.kr
Product data sheet
✔
Components |  | Composition (wt.%) |  | 
Structural carbohydrates | Glucan |  | 77.71±0.29 | 
 | Xylan |  | 0.93±0.07 | 
 | Mannan |  | 0.99±0.09 | 
 | Galactan |  | - | 
 | Arabinan |  | - | 
 |  | Subtotal | 79.63 | 
Lignin | Acid soluble |  | 4.33±0.08 | 
 | Acid insoluble |  | 18.23±0.22 | 
 |  | Subtotal | 22.56 | 
Analyzed by : Won Il Choi
Approved by : Hyun Jin Ryu
(sign)
2017년 06월 00일
주식회사 슈가엔