## Slide 1
Product information: Lot No. FMPT
Product type | Saccharomate Fractomass
Source Biomass | Pine tree (Korea)
Fractionation | H2SO4 aided organosolvent process
Data Report
Ⓡ
Ⓡ
Sugaren Co., Ltd. #B207, Seogwan, 152, jukjeon-ro, Suji-gu, Yongin-si, Gyeonggi-do, 16890, Korea
www.sugaren.co.kr
Tel. 031-8005-3549
Fax. 031-8021-7420
E-mail: sugaren@sugaren.co.kr
Product data sheet
✔
Components |  | Composition (wt.%) |  | 
Structural carbohydrates | Glucan |  | 9.15±0.18 | 
 | Xylan |  | 0.63±0.02 | 
 | Mannan |  | 0.52±0.07 | 
 | Galactan |  | - | 
 | Arabinan |  | - | 
 |  | Subtotal | 10.30 | 
Lignin | Acid soluble |  | 6.75±0.22 | 
 | Acid insoluble |  | 83.67±0.53 | 
 |  | Subtotal | 90.42 | 
Analyzed by : Won Il Choi
Approved by : Hyun Jin Ryu
(sign)
2017년 06월 00일
주식회사 슈가엔