## Slide 1
Sugaren Co., Ltd. #410, 2 Gwahakgwan, 119. Dandae-ro, Dongnam-gu, Cheonan-si, Chungcheongnam-do, 330-714, Korea
www.sugaren.co.kr
Tel. 041-529-6262
Fax. 041-559-7954
E-mail: sugaren@sugaren.co.kr
Analytical Report
Analytical results
Information
의뢰기관 | -
분석시료명 | Barley straw (Korea)
분석항목 | Total
Components |  | Composition (wt.%) |  | 
Structural carbohydrates | Glucan |  | 39.40±0.76 | 
 | Xylan |  | 16.25±0.23 | 
 | Mannan |  | 0.35±0.06 | 
 | Galactan |  | 0.92±0.11 | 
 | Arabinan |  | 2.23±0.10 | 
 |  | Subtotal | 59.15 | 
Lignin | Acid soluble |  | 0.87±0.08 | 
 | Acid insoluble |  | 16.61±0.18 | 
 |  | Subtotal | 17.48 | 
Extractives | Water |  | 15.43±0.73 | 
 | EtOH |  | 2.13±0.13 | 
 |  | Subtotal | 17.56 | 
Acetyl group |  |  | 0.91±0.13 | 
Ash |  |  | 7.11±0.04 | 
Total |  |  | 102.21 | 
본 성적서는 의뢰자가 제공한 시료의 분석 결과이며, 당 사의 사전 동의 없이 상업적 목적으로 하는 선전, 광고 및 법적자료로 사용될 수 없습니다.
Quantification was performed by following NREL laboratory analytical procedures: NREL/TP510-42618 (structural carbohydrates and lignin), NREL/TP510-42619 (Extractives), NREL/TP510-42622 (ash) and NREL/TP-510-42625 (protein).
Multi-replication have been conducted for test assay in carbohydrate (n=25). Q-Test was used to identify statistical outliers in data. Q-Test decision level at 95% confidence interval for N=25 is 0.317.
Analyzed by : Won Il Choi
Approved by : Hyun Jin Ryu
(sign)
2017년 06월 00일
주식회사 슈가엔