## Slide 1
Product information: Lot No. FMBS
Product type | Saccharomate Fractomass
Source Biomass | Barley straw (Korea)
Fractionation | H2SO4–catalyzed hydrothermal & Enzymatic hydrolysis process
Data Report
Ⓡ
Ⓡ
Sugaren Co., Ltd. #B207, Seogwan, 152, jukjeon-ro, Suji-gu, Yongin-si, Gyeonggi-do, 16890, Korea
www.sugaren.co.kr
Tel. 031-8005-3549
Fax. 031-8021-7420
E-mail: sugaren@sugaren.co.kr
Product data sheet
✔
Components |  | Composition (wt.%) |  | 
Structural carbohydrates | Glucan |  | 37.72±0.93 | 
 | Xylan |  | 2.23±0.20 | 
 | Mannan |  | 0.65±0.06 | 
 | Galactan |  | - | 
 | Arabinan |  | - | 
 |  | Subtotal | 40.60 | 
Lignin | Acid soluble |  | 1.08±0.03 | 
 | Acid insoluble |  | 51.74±0.57 | 
 |  | Subtotal | 52.82 | 
Analyzed by : Won Il Choi
Approved by : Hyun Jin Ryu
(sign)
2017년 06월 00일
주식회사 슈가엔